# Stainless-steel sluice gate

Square opening for wall-mounting with anchors (closed self-contained frame)

Shut-off and control valve for water and wastewater up to 50°C

Size 150x150 – 1000x1000, 4-10 mWC on-seat and off-seat

Compact valve type C (for non-flooded installation)

Sealing on four sides, for wall-mounting with anchors; tightness max. 1% (at on-seat pressure) and max. 5% (at off-seat pressure) of the permissible leak rate according to DIN 19569 Part 4 in installed state; including manufacturer’s inspection certificate to DIN EN 10204, 2.1, with specification of the leak rate;

Pressure ratings (on-seat and off-seat):

150x150,200x200   	10mWS

300x300			 8 mWS

400x400….800x800	 6 mWS

900x900,1000x1000	 4 mWS

Compact valve, self-contained frame structure, pre-assembled and ready for operation;

With fastening material (stainless steel A4 / AISI 316)

With non-rising stem and integrated stem bearing;

Sliding system between gate and frame

Vibration-free guiding of the gate over the entire travel; can be used in intermediate positions;

Integrated and chambered profile- seal made of waste-water and UV-resistant EPDM;

Seal between valve and wall made of waste-water resistant microcellular rubber; mounted to the valve and ready for operation;

Welded frame structure made of stainless steel A2 grade 304 – pickling bath treated and passivized;

Welded gate structure made of stainless steel A2 grade 304 – pickling bath treated and passivized;

stem with rolled trapezoidal thread made of stainless steel grade 431 (1.4057);

with rotatable stem nut made of sea-water and waste-water resistant bronze;

Sealing made of wastewater- and UV-resistant EPDM

Dimensions of the wall opening:	 ______ mm x ______ mm

On-seating operating pressure: 	____________ m WC

Off-seating operating pressure: 	____________ m WC

Installation depth:		____________ mm

(measured from the gate bottom to the operating gallery)

#### VAG ERI®plus Sluice Gate or equivalent

Manufacturer:	VAG GmbH

Carl-Reuther-Str. 1

68305 Mannheim

Germany

www.vag-group.com

Varieties:

- Version type O (open frame design) for flooded installation

- other (also rectangular) shapes

- Sealing on 3 sides for channel installation

- improver corrosion protection: frame and gate made from stainless steel A4 grade 316

- flexible installation with VAG REMO remote control system

- including manufacturer’s inspection certificate to DIN EN 10204, 2.1, with specification of the leak rate

Quantity ........   €/Piece .........   €/Item .........