Pull-Lock for PE-HD pipes
PN 16
DN 80 ... 200
two-part design

Consisting of:
-	Tension ring made of ductile iron EN-JS 1030 (GGG-40),

Corrosion protection:
Inside and outside epoxy-coated with GSK type “heavy-duty corrosion protection” to
DIN 30 677-2, coating thickness >250 µm, colour: RAL 5005 blue

	    -	Clamping ring made of white plastic circular-milled on the inside

VAG BAIO®stop Pull-Lock for PE-HD pipes or equivalent

Manufacturer:	VAG GmbH
		Carl-Reuther-Str. 1	
		68305 Mannheim
		Germany
		www.vag-group.com

Quantity ........    €/piece ........    €/item. .......